## Slide 1
Anubhav Roy
CNRS (UMR 7190) Sorbonne University
aroy_esm@psu.edu anubhav.roy@dalembert.upmc.fr
Cohesive zone Finite Element model for large scale yielding in fatigue

## Slide 2
MACRO
MICRO
Motivation: establish a multi-scale bridge.

## Slide 3
We leverage physics-based methods for residual lifetime prediction of critical components.
3

## Slide 4
Criterion:
Problem:
Linear Elastic Fracture Mechanics (LEFM) breakdown.
W: Structural Size
4
However, there are open questions.

## Slide 5
Objective: Investigate the doghouse shape within the walls of combustion chambers of CNES space shuttles subjected to fatigue.
Wall specimens containing a crack subjected to Mode–I fatigue
Number of Wall Specimens: 8
Specification for the fracture test:

## Slide 6
The effects of the length scale on the failure of CuCrZr are numerically investigated using Finite Element modelling.
Conditions * :
Model Dimensions:
Specimen# | h (in mm) | 
1 | 20 | 0.33
2 | 25 | 0.26
3 | 30 | 0.21
4 | 35 | 0.19
Specimen# | h (in mm) | 
1 | 20 | 0.33
2 | 25 | 0.26
3 | 30 | 0.21
4 | 35 | 0.19
*Li, Z., 1996. A new technique for determining fracture toughness KIC and its confidence with single DCB specimen. Engineering fracture mechanics, 55(1), pp.133-137.

## Slide 7
Materials have finite load bearing capacity
Input data: traction-separation law described by :
Cohesive stress
Separation
From which we deduce
measured by
statistical fractography
}
Force vs Displacement
The cohesive traction separation law is validated and used for the elastoplastic scenario.

## Slide 8
L
2h
Cohesive Zone
A cohesive zone model has been developed in Finite Elements.

## Slide 9
Specimen #4
Validation: A reasonably good agreement with theory validates the numerical simulations for brittle versions across sizes.
*Li, Z. (2014). A new technique for determining fracture toughness and its confidence with single DCB specimen. Engineering fracture mechanics, 55(1), pp.133-137.
Kanninen‘s* K vs a model for DCB
*Kanninen, M.F. (1973). An augmented double cantilever beam model for studying crack propagation and arrest. International Journal of Fracture, 9, pp. 83 - 92.
LEFM criterion at initiation for Specimen #4 (largest DCB)

## Slide 10
Result #1: The effects of the length scale on the failure of CuCrZr are numerically studied across specimen sizes.

## Slide 11
Results for #1: Distribution of the Von Mises Stress ahead of the crack tip for different specimens.

## Slide 12
Task #1: The effects of confined plasticity are studied for peak force and peak displacements as a ratio to the brittle scenario.

## Slide 13
Task #2: A scheme is designed to develop a bridge between points along the Paris Law and elastoplastic CZM.

## Slide 14
Step #1: Material characterization of the additively manufactured CuCrZr through uniaxial tensile testing of KBr specimens.
Extract elasticity parameters :
Establish Ramberg-Osgood parameters :

## Slide 15
Step #2: Catastrophic failure of the largest sample, Specimen 4 Sample 1 (Sp4.1) under monotonic loading.

## Slide 16
Goals for Step #2: Measure force-displacement behavior and perform statistical fractography.
DIC: instantaneous crack length a
Estimate Gc

## Slide 17
Step #3: Characterize C, m for Paris Law through low cycle fatigue.

## Slide 18
Step #4: Run FE simulations (with updated ) to prepare test protocols.

## Slide 19
Step #4 Idea: Visualizing fatigue as a series of monotonic loadings.

## Slide 20
Step #4 Idea: Visualizing fatigue as a series of monotonic loadings.

## Slide 21
*Seifi, R. and Hosseini, R., 2018. Experimental study of fatigue crack growth in raw and annealed pure copper with considering cyclic plastic effects. Theoretical and Applied Fracture Mechanics, 94, pp.1-9.
21
Protocol for Copper*

## Slide 29
Protocol |  |  |  |  |  | 
1 | 0.17 | 1/6 | 1.55 | 0.94 | 8826306 | 0
2 | 0.33 | 0.33 | 3.1 | 1.87 | 460671 | 0
3 | 0.5 | 0.5 | 4.6 | 2.8 | 81892 | 3.15
4 | 0.67 | 0.67 | 5.97 | 4.95 | 24043 | 10
5 | 0.83 | 0.83 | 6.89 | 9.63 | 9293 | 17.98
6 | 1 | 1 | 7.75 | 23.08 | 4274 | 26.68
Results for Copper